## Slide 1: Failure Mechanisms of Special Surfacings

## Slide 2: Non Slip Seal Coat – Christchurch Style

## Slide 6: Aftershocks total = 2086 May 6 2011

## Slide 7: Outline of Presentation
History
Failures
Modes of Failure
  Adhesive Failure
  Delamination Failure
  Cohesive failure
Pavement Design
Solutions
Conclusions

## Slide 8: History
Early 1960s rapid increase in traffic
Crashes increase – Black Spots identified
Focus on surface condition
Develop high friction surfaces
Shellgrip in Christchurch in Early 1990s

## Slide 9: HFS Failures
Application Failures
Adhesive failures and delamination usual failure modes
Existing surface contaminated
  Bitumen
  Road grime
  Moisture
Dirty Aggregate
Wrong weather
Cure too slow
Cure too fast

## Slide 10: Inconsistent binder application

## Slide 11: Trafficking before the binder cured

## Slide 12: Chip loss from dirty chip

## Slide 13: Delamination from water rising from below

## Slide 14: Delamination due to bitumen rich surface

## Slide 15: Delamination due to surface contamination

## Slide 16: Delamination due to surface contamination

## Slide 17: Cohesive Failure in asphalt

## Slide 18: HFS with Asphalt Attached
1-3mm Calcined Bauxite in Epoxy Binder.
AC14 Asphalt still attached to HFS

## Slide 19: Cohesive Failure – Moisture?

## Slide 20: Cohesive Failure within the asphalt
Possible causes
  Water build-up under the HFS strips the binder
  Expansion and contraction differentials
  Stiffness differences
  Shear stress too large
  Asphalt too weak

## Slide 21: Diagram depicting cohesive failure
Possible Cause 1
Water strips the binder
Reduces the internal friction of the asphalt
Asphalt fails at the high shear stress points

## Slide 22: Diagram depicting cohesive failure
Possible Cause 2
HFS expands and contract at different rate
Small differentials crack the bonds
Asphalt fails at the high shear stress points

## Slide 23: Diagram depicting cohesive failure
Possible Cause 3
HFS stiffer than asphalt
Asphalt deflects more breaking bonds
Asphalt fails at the high loading points

## Slide 24: Diagram depicting cohesive failure
Possible Cause 4
Shear stress is transmitted into the asphalt
The asphalt internal friction too low
The asphalt fails at the high shear stress points

## Slide 25: Diagram depicting cohesive failure
Possible Cause 5
Stress is transmitted into the asphalt by any or all of the above
The asphalt internal friction is too low
The asphalt fails

## Slide 26: Pavement Design
HFS used on high demand sites
HFS used instead of realigning sites with poor geometrics
High demand pavements
  International – 100mm AC on 200 – 300mm Structural Asphalt Pavement.
  New Zealand – 50mm AC on Unbound Granular Pavement
Starting to see some change to this.
NZ Economic Analysis does not include the cost of disruption to motorist or neighbours.
Cheaper to surface with high PSV aggregate in a thin asphalt surfacing than proper pavement and HFS

## Slide 27: Solutions
Better Pavements
Better Asphalt Design
Better Asphalt Binders
Better HFS Binder

## Slide 28: Better Pavements
Thick asphalt limits permeability
Thicker asphalt larger stone
Deeper stone anchors
Lower deflections less differential

## Slide 29: Better Asphalt Design
Larger stone deeper anchors
Increased internal friction
Increased tensile strength
Reduced permeability

## Slide 30: Better Asphalt Binders
Better asphalt internal friction
Asphalt handles stress better
Asphalt more durable when stressed
Binder more resistant to stripping

## Slide 31: Better HFS Binder
Binder breathes like the asphalt
Binder deflects and expands and contracts like the asphalt
Better adhesion properties
Better and faster curing binder

## Slide 32: Summary
Outlined the mechanisms of failure
Have offered some solutions
Still looking for the silver bullet
Any ideas to improve HFS lives welcomed

## Slide 33
Thank you for Listening